## Slide 1: Control of Semiconductor Spin Qubits Sorin P. Voinigescu, Suyash Pati Tripathi, Alireza Zandieh and Shai Bonen Edward S. Rogers Sr. Dept. of Electrical & Computer Engineering University of Toronto, Canada sorinv@ece.utoronto.ca September 14-18, 2020
Notes: I’d like to start this brief tutorial on the Control of Semiconductor Spin Qubits by acknowledging my graduate students Suyash, Alireza and Shai whose work is reflected in these slides, and GF for providing silicon fabrication through the 22FDX University Program

## Slide 2: Outline
Spin control basics
Biasing semiconductor qubits for quantum gate operation
Monolithic Quantum Processor (QP) proposals
Control circuit specification
Notes: I will begin with the spin control basics and discuss how to bias semiconductor qubits before covering several proposed QP architectures.
I’ll conclude with control circuit specification and the many research problems that still need to be solved.

## Slide 3: Control of a TLS
Qubit is pseudo spin
  Methods from nuclear magnetic resonance
Basic idea: Coherently rotate spin by static or oscillating magnetic fields
  Static field parallel to quantization axis => free precession, changes φ on Bloch sphere
  Oscillating field perpendicular to quantization axis => change population, i.e. change θ on Bloch sphere
  Readout of state = projection on Z-axis
Bloch sphere
θ
φ
y
x
z
|↑>, |0>
|↓>, |1>
|Ψ>
BDC
Bac
Notes: Irrespective of its implementation, the qubit behaves and is modelled as a pseudo spin.
Methods from nuclear magnetic resonance are applied to control it.
The basic idea is to coherently rotate the spin by applying static and oscillating magnetic fields.
The static field orientation defines the quantization axis, the Z-axis. It results in free precession of the spin state, PSI, around the Z-axis.
And changes the angle phi on the Bloch sphere.
The oscillating field is much smaller in amplitude and is applied perpendicular to the quantization axis.
By analogy with lasers, it changes the population occupancy of the Up or DOWN basis states which is equivalent to the angle theta changing on the Bloch sphere.
At the end of the sequence of quantum gate operations (i.e. at the end of the quantum algorithm) the final state of the spin is projected on the Z-axis collapsing into one of the two basis states: UP or DOWN, zero or one. This represents the readout operation.

## Slide 4: Spin ½ Hamiltonian in a rotating field
Notes: The mathematical framework for controlling the qubit is based on the Spin ½ Hamiltonian in a rotating magnetic field developed by Isidor Isaac Rabi in 1937 as part of his discovery of nuclear magnetic resonance for which he received the Nobel Prize in 1944.
An interesting and illuminating biographical detail: Rabi started out as an electrical engineering undergrad at Cornell University in upstate New York before switching to Chemistry and later to Physics as a graduate student.
He also worked on the magnetron before, and radar during, WWII. This perhaps explains how he came to use radio waves to probe the atom!
The behaviour of the single-spin qubit is described by a system of two coupled differential equations with respect to time, known as the Pauli equation, which is an extension of the Time-Dependent Schrodinger equation to include particle spin as well as the magnetic field.
The magnetic field B(t) consists of a large DC component, Bdc, along the Z-axis, and an ac field, B1, which can be decomposed in in-phase and quadrature components, rotating at angular frequency w in the x-y plane, perpendicular on the Z-axis.
Bdc defines the spin resonance, or Larmor, or qubit frequency, and B1 defines the Rabi frequency.
The dependence on magnetic field is linear for both characteristic frequencies.
B1<<Bdc
X(t) is a vector in the 2D Hilbert space with two complex components, a(t) and b(t), describing the evolution in time of the probabilities of finding the spin in the UP or DOWN basis state, respectively.

## Slide 5: Rotating wave approximation
[J.P.G. Van Dijk et al. PRA 2019]
Notes: How to control the qubit is best understood by recasting the Hamiltonian in the so-called rotating wave approximation, which ignores the second harmonic of the qubit nonlinearity at 2wo.
A matrix transform is used to obtain the Hamiltonian in the “rotating frame of B1” at frequency w, from the original ”lab frame” Hamiltonian.
sigma_z, sigma_x and sigma_y represent the 2x2 Pauli spin matrices, describing rotations around the x, y, and z-axes respectively.
For example, at spin resonance w=w_o, the first term is zero, meaning that no rotation occurs around the Z-axis.
To perform a rotation around the Z-axis, we can detune omega from omega_zero for a period of time corresponding to the desired rotation angle.
The speed of the rotation around the X and Y axes is set by omega_R and the phase of the carrier, phi, sets the rotation axis X or Y.
Finally, the evolution in time of the spin state is described by U.
“t” sets the duration of a particular rotation, therefore the angle of rotation.
The control signal can be synthesized using a radio transmitter architecture with linear I-Q modulator, like in modern 4G or 5G cellphones.

## Slide 6: Rotation angle: amplitude, time, phase
X-p/2
Y-p/2
Notes: The quantum gate operations consist of Larmor frequency pulses applied to the gate of the qubit.
The amplitude, duration and phase of the microwave pulses determine the angle and axis of rotation.
This example, is based on a verilogA model of the qubit Rabi equations in the lab frame.
An ac magnetic field, whose waveform is shown in the top panel, ais pplied along the X-axis, oscillating at w=w_0=100 GHz.
The initial state of the spin is on the equator at the intersection of the Y-axis with the sphere.
The projections of the spin state on the Z, X and Y axes are shown in the second, third and fourth panel, respectively.
The magnetic field produces first a 90-degree X-axis rotation, reaching the spin-UP basis state (at the NORTH POLE).
Next, by abruptly changing the phase of the carrier by 90-degrees in the middle of the time interval, B1 produces a 90-degree rotation around the Y-axis to bring the qubit state back on the equator, this time at the intersection with the the X-axis.

## Slide 7: Rotation angle: amplitude, phase, shape
X-p/2
Y-p/2
Notes: The same sequence of quantum gate operations is implemented here, but rather than using rectangular pulses to control the amplitude and phase of the qubit, gaussian pulses with identical duration and energy are employed. The Gaussian shape introduces less spectral spillover than rectangular pulses. This is particularly important for SC qubits and if FDM is employed.
The animation illustrates how the instantaneous amplitude of the gaussian pulse which modulates the carrier, affects the speed of the rotation on the Bloch sphere.
The question (which we shall answer later) is: how large can the amplitude be? We will see that it depends on qubit capacitance, DC characteristics, and DC magnetic field.

## Slide 8: Manipulation with oscillating B-field
[L.Hutin, IMS 2019 Short Course]
Notes: How is the ac magnetic field applied to the qubit?
It can be produced by passing an ac current through a transmission line which is closely coupled to the qubits we want to control.
The Rabi frequency becomes linearly proportional to the ac current.
This technique is know as ESR = electron spin resonance.
The problem with this approach is that it is difficult to apply locally to individual qubits.

## Slide 9: Manipulation with AC electric field
Notes: Ideally, we would want to drive the qubit using a variable electric field.
This technique, known among physicists as Electron Dipole Spin Resonance (EDSR) can be accomplished by applying an ac-voltage on the gate of the qubit (MOSFET).
In this case, the Rabi frequency depends linear on the amplitude of the AC voltage applied to the gate. Small amplitudes must be used to satisfy small signal conditions and avoid exciting other energy levels/electrons.
Unfortunately, this scheme works for hole-qubits only.
For electron-spin qubits a gradient in the magnetic field is also needed. The gradient magnetic field is obtained by integrating a micromagnet, not an easily scalable proposition.

## Slide 10: Outline
Spin control basics
Biasing semiconductor qubits for quantum gate operation
Monolithic Quantum Processor (QP) proposals
Control circuit specification
Notes: In order to control the qubit and perform a quantum gate operation, we must first learn how to bias the qubit!

## Slide 11: FDSOI vs. FinFET spin qubits
[R. Pillarisetty et al., IEDM 2019]
1x18nmx70nm FDSOI p-QD
Notes: With semiconductor qubits, we do so in the subthreshold triode region.
The transfer characteristics of FDSOI hole and FinFET electron quantum dots biased in the triode region at low VDS and measured at cryogenic temperatures exhibit current peaks and troughs in the subthreshold region.
These are manifestations of Coulomb blockade, with the first peak at VGS=-0.47V and 1.15V, respectively corresponding to the first energy level in the quantum dot being occupied by a single hole/electron, respectively.
The next peak, corresponding to VGS=-0.525 V and 1.23 V, respectively, indicates that a second hole/electron of opposite spin has been added to the energy level.
In these examples, the ac voltage amplitude applied on the gate must therefore be smaller than half the peak-to-peak spacing (35mV) to avoid adding a second hole/electron to the dot. Small signal conditions may dictate even smaller amplitudes.

## Slide 12: FDSOI vs. FinFET spin qubits
1x18nmx70nm p-QD
FDSOI
FINFET 10 mK
[R. Pillarisetty et al., IEDM 2019]
Notes: By repeating the transfer characteristics measurements at different VDS values one obtains the current “diamonds” in the VDS-VGS plane.
The larger the dark region of the first diamond (occupied by one hole/electron), the larger the SNR and the more design margin is available to the DAC that must provide the bias of the qubit.
Wider diamonds at higher temperatures indicative of a more robust qubit that operates at higher temperature and requires a lower resolution DAC for the gate bias.
Nevertheless, the resolution of the DAC that controls the VDS of the qubit must be sufficient to resolve the Zeeman energy split produced by BDC, typically in the 100uV to 300uV range.
Important note: For monolithic processors, the qubit technology must be in an FDSOI or FinFET CMOS node with undoped channel, avoiding impurity deionization problems, suitable for operation at cryogenic temperature, and which at can accommodate the microwave or mm-wave control electronics.
FDSOI has the added benefit of the backgate which can be used to correct the significant threshold voltage variation from room temperature.

## Slide 13: The 1-qubit QP as a nonlinear mixer
ω0 = 80 GHz
ωR = 4 GHz
[M. Gong et al. RFIC 2019]
Qubit with readout quantum dot form a cascode
biased in the subthreshold triode region
ωR = 4 GHz
Readout amplifier
Notes: This slide summarizes the behaviour of the qubit in the rotating frame as a non-linear device, similarly to that of a downconvert mixer.
A carrier signal is applied continuously on the left of the slide at the spin resonance frequency to the input of the qubit to perform a quantum gate operation. In this example the frequency is 80 GHz for operation at 4 K.
As shown at the bottom left of the slide, the resulting gate operation is a continuous rotation on the Bloch sphere around the X-axis.
Whenever the spin reaches the South Pole, an electron is detected by spin-to-charge conversion and its signal is amplified by a low-noise readout amplifier. Assuming error-free readout and instantaneous tunnelling, this event occurs with the periodicity of the Rabi frequency.
The Rabi oscillation (4 GHz in this case) is illustrated at the drain of the qubit at the top of the slide and amplified at the output of a low noise readout amplifier.
A larger amplitude of the 80-GHz carrier on the left leads to a higher Rabi frequency and a faster quantum processor.
In summary, the quantum computer can be regarded as an Analog Mixed Signal Circuit operating in 2D real space, with variables theta and phi, with the result collapsing to 0 or 1.
The spin manipulation frequency is the highest frequency signal in the system and acts as reference for all the other signals and activities in the QP, while the much lower Rabi frequency acts as the clock frequency of the quantum gate and quantum processor.

## Slide 14: Outline
Spin control basics
Biasing semiconductor qubits for quantum gate operation
Monolithic QP proposals
Control circuit specification
Notes: Let us now briefly review the architectures of recently proposed monolithic quantum processors.
It should be noted, however, that none of them has been fully demonstrated yet.

## Slide 15: Linear Upconversion Monolithic QPs
[B. Patra et al., ISSCC 2020]
Google, Microsoft, TU Delft + Intel's
U of T, Equal1, LETI
Notes: In state-of-the-art SC QPs, the electronic controller synthesizes, individually for each qubit, an ultra-low phase noise, pulse-modulated microwave carrier at ω0, obtained by linear IQ upconversion similar to a 4G or 5G radio transmitter.
The ultimate goal is to integrate the controller and qubit array on the same die. This is only possible at higher temperature, above 100 mK, but is still limited by the power consumption of the control electronics and the thermal lift of the cryostat. The higher the temperature, the higher the cryostat thermal lift and the higher the integration level. At this time, a 3-Kelvin monolithic quantum processor with hundreds-to-thousands of qubits and associated control electronics looks achievable.

## Slide 16: Muxing Control (FDM) and Readout
[D. Riste et al., IEEE Microwave Magazine, Aug.2020]
[M. Jerger et al., J.Appl. Phys., 2012]
Notes: Several schemes have been proposed to reduce the number of control and readout circuits.
As shown on the left, at the very least, the Larmor frequency LO source can be shared by all qubits.
Additionally groups of qubits could be time-interleaved to share one upconverter. However, time-interleaving commensurately reduces the depth of the quantum algorithm that can be executed within the lifetime of a qubit.
The control and readout electronics and the power consumption per qubit can be further reduced by sharing a control line and a readout line between several qubits. For example, 9 readout resonators share the same readout line and amplifier in the case of Google’s 54 qubit SC QP.
The FDM control scheme was proposed in the early twentyteens for SC processors.
While this scheme has worked well for readout because it occurs after all gate operations have been completed, it is very problematic for control for two reasons:
the control subcarrier signal tuned to the spin resonance frequency of one qubit acts as aggressor for the other qubits causing parasitic rotations.
It is very difficult to physically implement semiconductor qubits with widely different resonance frequencies. On-chip magnets with non-standard back-end of line, more control lines and/or increased more power consumption will be needed.

## Slide 17: Direct Modulation Monolithic QP
Qubit array
  Pdc =5 pW (10pA/50mV) per qubit
  1010 qubits = 5 mW
Spin manipulation
  low phase noise (OFDM) signal at fL
  60-100 GHz for 3-5 K operation
  140-240 GHz for 8-12 K operation
  n-MOSFET switch+phase pulse modulators
SRAM stores digital pulse sequences (gate operations)
Control/readout circuits dominate consumption. Integration limited by cryostat lift
Note: qubit bias scheme not shown
[S. Bonen et al. EDL 2019]
Notes: A different architecture, similar to that of an RF DAC, is shown on this slide and has been proposed for operation at temperatures above 3 K.
The low-phase noise mm-wave carrier, in the 60-240 GHz range, is directly modulated in phase and amplitude using MOSFET switches which consume no power.
As we can calculate from the measured transfer characteristics shown earlier, the qubit itself, consumes less than 5 pW. This means that as many as 10 Billion qubits can be integrated on a die within a 5mW power budget.
The 80-GHz Phase Locked Loop consumes 300 mW and can be integrated on chip along with the SRAM which stores the digital pulse sequences for quantum gate operations.
The formidable challenge is for the Analog-Mixed-Signal mm-wave electronics to be be kept within a power budget of less than 2-3W at 3-4 K.
This translates to less than 3-4uW per qubit in a QP with 1 million qubits.
Quantum processors with 1000 qubits co-integrated with control electronics, operating at 3-4 K, look quite feasible in today’s production 22nm FDSOI CMOS.

## Slide 18: 100mK AMS QP in 28nm FDSOI
[L. Le Guevel et al., ISSCC 2020]
Notes: This slide shows a similar architecture and approach but at much lower frequencies (~3 GHz) and temperatures of 100 mK in 28nm FDSOI.
In this case the carrier amplitude is controlled individually per qubit using capacitive DACs.

## Slide 19: AMS Charge QP in 22nm FDSOI
[D. Leipold, et al. 2019]
Notes: Finally, this slide shows a monolithic QP architecture based on semiconductor charge qubits and fast switching capacitive DACs.
The quantum core is controlled used GS/s DACs and the result of the quantum algorithm are read using single-electron detectors and switched-capacitor amplifiers.

## Slide 20: Quantum Core and Control Detail
  [I. Bashir et al., IEEE SSC-L, Sep. 2020]
Notes: A Scanning Electron Microscope picture of the quantum core layout consisting of two coupled qubit arrays using minimum size 22nm FDSOI MOSFETs is shown on the left, while the control circuit schematics, based as GS/s DACs is provided on the right side.

## Slide 21: Outline
Spin control basics
Biasing semiconductor qubits for quantum gate operation
Monolithic QP proposals
Control circuit specification
Notes: Finally, how should the control electronics be specified?

## Slide 22
Control circuit provides
Sorin P. Voinigescu
[Keysight, EuMW 2018 Short Course]
Notes: Let’s first review what the control circuit must provide

## Slide 23
Qubit bias state for initialization, manipulation and readout => DAC with moderate speed ~fRabi
Control circuit provides
Sorin P. Voinigescu
[Keysight, EuMW 2018 Short Course]

## Slide 24
Qubit bias state for initialization, manipulation and readout => DAC with moderate speed ~fRabi
Low phase-noise, pulse-modulated (FDM) spin-manipulation signal at microwave or mm-wave frequency ~fLarmor
Control circuit provides
Sorin P. Voinigescu
[Keysight, EuMW 2018 Short Course]

## Slide 25
Qubit bias state for initialization, manipulation and readout => DAC with moderate speed ~fRabi
Low phase-noise, pulse-modulated (FDM) spin-manipulation signal at microwave or mm-wave frequency ~fLarmor
Low-noise readout
Control circuit provides
Sorin P. Voinigescu
[Keysight, EuMW 2018 Short Course]

## Slide 26
Qubit bias state for initialization, manipulation and readout => DAC with moderate speed ~fRabi
Low phase-noise, pulse-modulated (FDM) spin-manipulation signal at microwave or mm-wave frequency ~fLarmor
Low-noise readout
Synchronization of the above signals
Control circuit provides
Sorin P. Voinigescu
[Keysight, EuMW 2018 Short Course]

## Slide 27
Carrier frequency (fLarmor) accuracy, phase noise, and amplitude accuracy, PLL bandwidth (~4*fRabi)
Control circuit specification
Sorin P. Voinigescu
Notes: What must be specified for the control circuit?
First, the precision of the carrier frequency which must be equal to the Larmor frequency during spin manipulation.
Second, Its phase noise and integrated jitter over the duration of the quantum gate operation: e.g. ½ Rabi period for pi-rotations or ¼ of the Rabi period for pi/4 rotations.
Third, we must specify the carrier amplitude and its accuracy which determines the Rabi frequency.
The challenge is that the amplitude required to control a qubit is different for each qubit implementation and musty be determined from complex measurements at cryogenic temperatures.

## Slide 28: Carrier accuracy specification
Quantum Gate Error
larmor
Relative Error of Circuit Parameter
Notes: For example: To keep quantum gate errors below 10-5, both the carrier frequency and its amplitude must be controlled with better than 0.3% error.
The rms phase error must be lower than 0.2 degree.
This demands and RF DAC with >8-bit accuracy, or a linear upconverter of equivalent resolution and phase noise.

## Slide 29: Example 22nm FDSOI 80GHz PLL PN
300 K
RMS phase error (10 KHz to 100 MHz) = 0.23 degree
Notes: These specs, tougher than for 5G radio, are now achievable in 22 nm FDSOI CMOS, even at 80 GHz, as these measurements of an 80-GHz PLL demonstrate, even at room temperature.

## Slide 30
Carrier frequency (fLarmor) accuracy, phase noise, and amplitude accuracy, PLL bandwidth (~4*fRabi)
Bias DAC range, precision, noise, bandwidth (~fRabi)
Control circuit specification
Sorin P. Voinigescu
Notes: Next comes the specification of the bias DAC in terms of output voltage range, precision, noise and bandwidth. The latter must be on the order of the Rabi frequency.

## Slide 31
Gate (drain/source) bias
Range: 0-800 (50) mV & Resolution: 0.1 mV => 13 (9) bits
Speed> 4xfRabi = 400 MHz
Power consumption
Size
Noise < LSB/10 > Cstorage > 660 fF
18nmx50nm qubit capacitances: CGS=10aF, CGD= 10aF, CDB=2.5aF
4K Bias DAC specification
Sorin P. Voinigescu
DAC type and SSC-L paper | range | LSB | res | PDC/Speed
GaAs spin, charge redistribution [Vliex] | 0-1 V | 250 mV | 13 bit | 2.7 mW/
28nm FDSOI spin, current steering [Zurita] | 0-6.6 mV | 26 mV | 8 bit | 7 mW/ 100MS/s
22nm FDSOI charge, charge redistribution [Esmailiyan] | 0-70 mV | 300 mV | 8 bit | 270 mW/ 2GS/s
Notes: This slide shows examples of cryogenic DACs from the September 2020 issue of the IEEE SSC-L.
To achieve the 0-800 mV range with 100uV resolution, as needed for FDSOI qubits, at least 13 bits are required.
The range is even larger in experimental qubit technologies such as those based on GaAs quantum dots or Si/SiGe FinFET quantum dots.
To relax the resolution spec, a scheme has been proposed where a DAC with a larger voltage range is used for coarse setting and is combined with a second, finer resolution DAC, for precision setting.
The bias voltage must be switched at hundreds of MHz, dictating the speed of the bias DAC.
Its power consumption and size must be as small as possible to enable large integration levels.
Ideally, the DAC size should be comparable to that of the qubit but is usually limited by the size of the storage capacitor which must be large enough to reduce noise below the LSB level.
The table at the bottom of the slide compares the performance of three ESSCIRC 2020 cryogenic DACs designed for biasing Si or GaAs qubits.

## Slide 32
Carrier frequency (fLarmor) accuracy, phase noise, and amplitude accuracy, PLL bandwidth (~4*fRabi)
Bias DAC precision, range, noise, bandwidth (~fRabi)
Switch isolation, modulation bandwidth (~4*fRabi)
Control circuit specification
Sorin P. Voinigescu
Notes: In the case of the architecture with direct pulse modulation of the carrier frequency, the switch must have >40 dB isolation to prevent parasitic modulation of idle qubits by the signal applied to those qubits on which gate operations are performed at a given moment.
The modulation bandwidth of the switch must be larger than 4x F-Rabi. Even 40 GHz is easily achievable in today’s FDSOI or FinFET CMOS technologies.

## Slide 33
Carrier frequency (fLarmor) accuracy, phase noise, and amplitude accuracy, PLL bandwidth (~4*fRabi)
Bias DAC precision, range, noise, bandwidth (~fRabi)
Switch isolation, modulation bandwidth (~4*fRabi)
Crosstalk (< -45 dB)
Control circuit specification
Sorin P. Voinigescu
Notes: Related and more of a problem than switch isolation, qubit-to-qubit crosstalk is present in all semiconductor qubit cores and is unavoidable.
For example, a crosstalk of 20 dB causes parasitic gate rotations of 9 degree in neighbouring qubits if a 90-degree rotation is performed on the aggressor qubit.
Like switch isolation, crosstalk is deterministic, can be characterized for each quantum core topology/layout, and likely compensated for by signal processing techniques.

## Slide 34
Carrier frequency (fLarmor) accuracy, phase noise, and amplitude accuracy, PLL bandwidth (~4*fRabi)
DAC precision, range, noise, bandwidth (~fRabi)
Switch isolation, modulation bandwidth (~4*fRabi)
Crosstalk (< -45 dB)
LO leakage (<-45 dB), SFDR ( >45 dB)
Subcarrier frequency spacing, Df, in case of FDM
Control circuit specification
Sorin P. Voinigescu
Notes: LO leakage and FDM produce similar unintended parasitic rotations on qubits which share the same control line and must be kept below 45-50 dB for error rates below 10-5.

## Slide 35: Impact of FDM & LO leakage
Notes: The problem with frequency–division multiplex control is illustrated here, where we see that the error introduced by one of the off-tune subcarriers on a particular qubit depends on the ratio between the subcarrier spacing and the Rabi rather than Larmor frequency.
For 10-5 error, the subcarrier spacing must be 300 times larger than the Rabi frequency!

## Slide 36: 5 carriers applied simultaneously
fRabi=100MHz
fLarmor=100GHz
Notes: This example illustrates a 5-qubit processor with the individual qubits tuned on 90, 95,100,105 110 GHz all having a Rabi frequency of 100 MHz.
The time domain waveforms and corresponding spectrum of the FDM spin manipulation signal applied at the input the qubits are shown in the top row.
The nonlinear behaviour is immediately apparent in the Fourier transform spectrum of the Z-axis projection of the 100GHz qubit, shown at the bottom right. The time domain waveform at the bottom left appears like a Rabi frequency sinusoid sampled at the Larmor frequency.
Tones due to the other subcarriers are also “downconverted”, albeit with decreasing amplitude for those spaced farther away.
The intermodulation products of all 5 subcarriers at the second harmonic around 200 GHz are also present, very much like in a multitone fibreoptic receiver or OFDM radio.

## Slide 37: Impact of number of subcarriers
At given error
more subcarriers
lead to lower
Rabi frequency
and small depth
algorithms!
Notes: Finally, it should be noted that the closest carrier has the largest impact and that the error does increase with the number of subcarriers.
Therefore, , when using FDM, for a given error rate, control circuit technology and circuit bandwidth one has to reduce the Rabi frequency and, as a result, the depth of the processor.

## Slide 38
Carrier frequency (fLarmor) accuracy, phase noise, and amplitude accuracy, PLL bandwidth (~4*fRabi)
DAC precision, range, noise, bandwidth (~fRabi)
Switch isolation, modulation bandwidth (~4*fRabi)
Crosstalk (< -45 dB)
LO leakage (<-45 dB), SFDR ( >45 dB)
Subcarrier frequency spacing in case of FDM
Readout amplifier gain, noise, bandwidth (~4*fRabi)
Control circuit specification
Sorin P. Voinigescu
Notes: Finally, for the readout operation, the amplifier noise, gain and bandwidth, also on the order of 4xf_Rabi, must be specified. Readout was not covered in this presentation.

## Slide 39
Strong crosstalk between <100nm spaced spin qubits => correction needed
FDM requires lower Rabi frequency => reduced algorithm depth
Difficult to tune semiconductor spin qubit frequency by over 10%
Size of bias capacitors
Fast readout
Readout resonators (if used) require large area
Challenges for control electronics
Sorin P. Voinigescu
Notes: In summary, what are the challenges and research problems that still need to be solved?
The strong crosstalk due to capacitive coupling between qubits spaced closer than 100 nm is unavoidable.
A correction method must be found to solve it.
Using frequency division multiplex techniques to reduce the number of control lines and control circuits demands a reduction of the Rabi frequency and, consequently of the quantum processor speed. This limits the depth (complexity) of the algorithms which can be run within the lifetime of the qubit.
For FDM, qubits tuned on widely different resonance frequencies must be integrated side by side, requiring CMOS process changes and/or qubit architecture innovation.
The size of the bias DAC and storage capacitor are much larger than that of qubit. In fact, the qubit is the smallest transistor in the technology, everything else is larger. Further miniaturization of the electronics is needed but it is not trivial.
Although I have not addressed readout, fast readout is necessary for error correction. Fast readout techniques have yet to be demonstrated for semiconductor qubits.
Some hope is placed in mimicking the SC qubit approach with narrow band readout resonators. Resonators need inductors which are even larger than capacitors.

## Slide 40: Papers to See This Year
Papers accepted in special ESSCIRC2020 issue of IEEE SSC-L
Cryogenic DACs:
  P. Vliex, et al.
  M.E.P.V. Zurita, et al.
  A. Esmailiyan, et al.
Cryogenic voltage reference: Y. Yang et al.
Cryogenic CMOS Library: E. Schriek et al.
Single-electron injection device for charge qubits: I. Bashir, et al.
Notes: I’d like to end by drawing your attention to the papers accepted …
Thank you.

## Slide 41: References (i)
R. Gross et al., “Physics of superconducting quantum circuits,” TU Munich course notes/slides 2001-2018.
I. I. Rabi, “Space Quantization in a Gyrating Magnetic Field,” Phys. Rev. 51 (1937), 652.
J. Bardin et al., “Quantum Computing,” IEEE Micro. Mag., pp.24-44, Aug. 2020.
D. Riste, et al., “Microwave Techniques for Quantum Computers,” IEEE Micro. Mag., pp.60-71, Aug. 2020.
J. P. G. Van Dijk et al., “The impact of classical control electronics on qubit fidelity,” Phys. Rev. Applied 12, pp. 044054, 2019.
M. Babaie, “Cryo-CMOS Circuits and Systems for Scalable Quantum Computing”, EuMW Conference Short Course, Sep. 2018.
J. Bardin, et al. “Design and Characterization of a 28-nm Bulk-CMOS Cryogenic Quantum Controller Dissipating Less Than 2 mW at 3 K,” IEEE JSSC, pp.3043-3060, Nov. 2019.
B. Patra et al., “A Scalable Cryo-CMOS 2-to-20GHz Digitally Intensive Controller for 4x32 Frequency Multiplexed Spin Qubits/Transmons in 22nm FinFET Technology for Quantum Computers,” IEEE ISSCC Digest, pp.304-305, Feb. 2020.
L. Le Guevel et al., “A 110mK 295μW 28nm FDSOI CMOS Quantum Integrated Circuit with a 2.8GHz Excitation and nA Current Sensing of an On-Chip Double Quantum Dot,” IEEE ISSCC Digest, pp.306-307, Feb. 2020.
L. Hutin, “Si MOS-Based Spin Qubits for Quantum Computing,” Short Course IMS 2019, June. 2019.
S. Bonen et al., “Cryogenic Characterization of 22nm FDSOI CMOS Technology for Quantum Computing ICs,” IEEE EDL, Vol. 40, No.1, pp.127-130, Jan. 2019.
R. Pillarisetty et al., IEDM, Dec. 2019.

## Slide 42: References (ii)
M.J. Gong et al., “Design Considerations for Spin Readout Amplifiers in Monolithically Integrated Semiconductor Quantum Processors,” IEEE RFIC, June 2019.
M. Jerger, et al., “Frequency division multiplexing readout and simultaneous manipulation of an array of flux qubits,” Appl. Phys. Lett., vol.101, no. 4, p. 042604, July 2012. doi: 10.1063/1.4739454.
L. Petit et al., “Universal quantum logic in hot silicon qubits,” Nature Vol.580, pp.355-360, April 16 2020.
A. Zandieh, et al., “128-GS/s ADC Front-End with over 60-GHz Input Bandwidth in 22-nm Si/SiGe FDSOI CMOS,” IEEE BCICTS, Oct. 2018.